## Slide 1: Integrated APC-GAN and AttuNet framework for automated pavement crack pixel-level segmentation: A new solution to small training datasets
Comprehensive Exam
by
Tianjie Zhang
Advisory Committee
Yang Lu, Ph.D.
Nick Hudyma, Ph.D.
Dave Zhai, Ph.D.
Alejandro Rosales, MS
May 6, 2022
Notes: Thanks advisory committee, other faculty, guests, and students.

## Slide 2
Background and Motivation
Research Goals
Proposed Research
Methodology
Preliminary Results
Emphasis Area: Data Science
Notes: Speak out all points

## Slide 3: Introduction
Crack has become one of the primary defects in pavement, which seriously affects the service life of pavement.
From: Deep Crack
Traditional inspection:
Pavement Crack
Cons:
Time-consuming
Labor-intensive
Dangerous
Affect Traffic Flow
From:https://www.fhwa.dot.gov/publications/research/infrastructure/pavements/ltpp/15049/007.cfm
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 4: Introduction
Intelligent pavement detection
and identification becomes a significant task.
The training dataset is lacking or uneven, making it insufficient to train an accurate segmentation model.
From: https://www.surveylegend.com/customer-insight/open-ended-survey-questions/
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 5: Introduction
In 2014, Goodfellow proposed the concept of generative adversarial networks (GANs), which can produce real-like images through a battle between a generator and discriminator.
Alec Radford proposed deep convolutional generative adversarial networks (DCGANs) based on the conception of GAN, and it showed good representations of images.
Data augmentation
Trad image-Aug
GAN
DCGAN
Crop, Flip, Adjust brightness, contrast, blur…
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 6: Introduction
The main idea of U-Net is to replace pooling operators by upsampling operators to increase the output resolution. Also, it combines the high-resolution features with the upsampled output to learn more precise information based on small dataset.
Bang, S et al. used ResNet-152 to increase the layers in structure in purpose of increasing the accuracy of cracks identification.
Network Structure
U-Net
Resnet
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 7: Introduction
This paper proposed a framework for pavement crack segmentation which contains an automated pavement crack generative adversarial network (APC-GAN) and a new pixel-level pavement crack segmentation network, AttuNet.
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 8: Data
A DeepCrack dataset was utilized in this work to test the performance of the CNN networks. The DeepCrack dataset is an open-source dataset published in GitHub (https://github.com/yhlleo/DeepCrack).
This dataset consists of 537 RGB crack images with manually annotated segmentations. The image has a resolution of 544 * 384 pixels.
The images are divided into two subsets:
300 images for training
237 images for testing.
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 9: APC-GAN
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 10: AttuNet
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 11: AttuNet
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 12: AttuNet
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 13: AttuNet
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 14: AttuNet
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 15: AttuNet
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 16: AttuNet
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 17: AttuNet
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 18: AttuNet
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 19: AttuNet
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 20: Background
Pavement distresses:
Cracking
alligator
transverse
block
longitudinal
Patching
Sealing
Manholes
Intelligent pavement detection
and identification becomes a significant task.
From: DSPS22
Pavement Distress
Traditional inspection: Time-consuming, Labor-intensive, Dangerous, Affect Traffic
Notes: First, let me introduce the background of this project.
There are several different pavement distresses, such as various cracks, patching, sealing, that occur over the course of a pavement’s service life and can negatively impact the performance and longevity of the structure lifespan. These distresses can occur as a result of loading, environmental conditions, chemicals, and materials used.
The traditional method to determine the number, type, and distribution of defects is often achieved by engineers identifying and counting them manually. However, this method is time consuming, labor intensive and also sometimes dangerous, as it affects the traffic.
A promising new field of interdisciplinary work with computer science being applied to the civil engineering industry, is intelligent pavement defect inspection and identification. If this method is implemented correctly, it could be utilized to identify pavement defects, the severity of the distress, and implement repairs; all through nondestructive methods.

## Slide 21
Notes: Speak out all points

## Slide 22: Pavement
What is Pavement:
Transportation capabilities
Goods, people, materials…
Often with vehicle
Application:
Roads
Freeways
Biking and walking
Transportation means between two places
Components of Surface Layer:
Aggregate
Asphalt Binder
Notes: As we are all familiar at this point, pavement is the structure used to transport materials, goods, or people to different locations, often with vehicles of some sort.

## Slide 23: Mix Design
Mix influences
  Aggregate properties
  Air voids
  Asphalt content
Mix verification
  Theoretical Max Specific Gravity (Gmm)
  Bulk Specfic Gravity (Gsb)
Notes: all of these factors have a big influence on the mix performance.
Superpave was developed in 1984 to improve the
uses volumetric verification, such as specific gravity, air voids, absorption, etc..

## Slide 24: Mix Design - SuperPave
Marshall Mix Design
SuperPave
  Superior Performing Asphalt Pavements (1984)
  Volumetric verification
    Target AC @ 4% air voids
  Superpave Gyratory Compactor (SGC)
  Predictive Performance Engineered Mix Design

## Slide 26: SuperPave Performance Grading

## Slide 27: Mix Design – BMD
Balanced Mix Design (BMD)
  Index based Performance Engineered Mix Design
  Volumetric + performance verification
  Performance testing
    Cracking
    Rutting
** Good performance vs. good mix characteristics **

## Slide 28: BMD Benefits
Volumetric Problems:
  Specific criteria
    Overlay applications
    Mix location
  New/recycled material
  Optimum performance
BMD solutions:
  Extend/optimize service life
  Climate Change
  Economic savings
    Cheaper binder + improved mix properties

## Slide 29: RAP and it’s contribution
Recycled Asphalt Pavement (RAP)
Milling and crushing existing roads
Surface AC 100% recyclable!
Available aged RAP binder
Recycled aggregate
RAP benefits
Economic
Environmental
Notes: These are concrete characteristics
Speak out all points in brief
*Can be skipped in the concrete specialized presentation

## Slide 30: Challenges and Solutions
Problems with High RAP
  Variability – source and properties
  Available aged RAP binder
  Gradation
  Cracking
  Rutting
Rejuvenators
  Revitalizes aged RAP binder
  Degree of dispersion/blending

## Slide 32: RAP + Rejuvenator uncertainty
RAP binder
  Available aged binder
  RAP binder properties
    Oxidation maltenes fuse asphaltenes
    Increase stiffness, less ductile
    low in oily maltenes
    high in very stiff asphaltenes
Rejuvenator
  Softens RAP binder
  Degree of blending
  Binder activation
  Perform as intended
Notes: High amount of uncertainty associated with high RAP mixes.
maltenes - the ‘glue’ portion of the pavement mix
asphaltenes - responsible for pavement rigidity

## Slide 33: Current Practice
‘High’ Recycled Asphalt Pavement (RAP)
  0-17% RAP No adjustment needed
  17-30% RAP Bump binder grade down one
  30% RAP and above need blending chart (‘High’ RAP)
ITD
  Upto 30% RAP replacement allowed
  No limit previously field problems

## Slide 34: Performance Testing - HWTT
Hamburg Wheel Tracking Test (HWTT)
Water bath @ 50℃
703 + 4.5 N force
< 10 mm rut depth within 15,000 passes
20,000 total passes
150 mm diameter, 62 mm height
Air voids: 7% + 0.5%
Notes: ** include brief history of other tests

## Slide 35: Performance Testing - IDEAL-CT
Indirect Tension Asphalt Cracking Test (IDEAL-CT)
Input sample parameters and dimensions
Displacement: 50 + 2 mm/min
Intermediate temp: 5℃ - 35℃
Load vs. Deformation with time curve
Output CTindex - cracking resistance
Benefits!

## Slide 36
Research Goals
Notes: Speak out all points

## Slide 37: Research Goals and Questions
Evaluate the effect of rejuvenators in improving the performance of asphalt mixtures with high RAP contents.
Do the rejuvenators effectively soften and blend with the aged RAP binder to reach a balanced mix?
2. Apply Balanced Mix Design (BMD) to optimize mix performance.
Does implementing a BMD for high RAP mixes prove to be an effective method of mix design?
3. Study economic savings from using rejuvenators and high RAP.
Does the use of rejuvenators in high RAP mix have significant economic benefits? If so, how much?
4. Develop thresholds for performance testing with high RAP mixes.
Are the current ITD performance thresholds reasonable? What should they be adjusted to and why? Specifically IDEAL-CT.

## Slide 38
Proposed Research
Notes: Speak out all points

## Slide 39
Literature Review
Materials Testing
Virgin Aggregate
Virgin Asphalt
RAP
Rejuvenators
RA1/RA2 dose
Blending Charts
Available Asphalt
HMA Mix
Design
Proposed Research Plan Part One
Gradation

## Slide 40
Proposed Research Part Two
HMA Mix Design
Virgin/Control Mix Design
Asphalt Content (%)
Mix Gradation
RAP Mix Design
25% RAP
50% RAP
70% RAP
100% RAP
RA1 &
RA2
PG 64-34
IDEAL-CT & HWTT Results

## Slide 41
IDEAL-CT &
HWTT Results
Proposed Research Part Three
Virgin/Control
Results
RAP Mix
Results
Compare
Data
Analysis
Trends
Duplicates
Future
Research

## Slide 42: Project Scope
Starting point:
  RAP percentages: 0% (control), 25%, 50%, 70%, 100%
  Virgin Asphalt: PG 70-28
RAP properties:
  RAP: PG 82-16
  Available AC = 5.3%
2 rejuvenators:
  1 bio-based (RA1) dose = 8.3% (weight of RAP)
  1 petroleum based (RA2) dose = 11.3 % (weight of RAP)
  (+1 other blend if time permits)
Performance test parameters:
  Rutting (HWTT)
  Cracking (IDEAL-CT)

## Slide 43: Key Consistencies
Overall AC = 5.3%
Virgin Binder = PG 70-28
Gradation:

## Slide 44: Testing matrix - Performance
Table 1: Testing Matrix Performance Testing Plan |  | 
 | RA 1 | RA 2
0% (control / virgin) | — | —
25% RAP - with RA’s |  | 
25% RAP - with PG 64-34 | — | —
50% RAP |  | 
70% RAP |  | 
HWTT - requires 4 samples (62 mm height, 7.0 + 0.5% air voids)
IDEAL-CT - requires 3 samples average (7.0 + 0.5% air voids)
Total samples- 56 samples

## Slide 45: Asphalt Binder Blend Testing
Table 2: Binder Blend Testing |  |  | 
 | Blend1 (RA1 + RAP binder) | Blend2 (RA2 + RAP binder) | Virgin Binder
BBR:m-value |  |  | 
DSR:G*/sin(𝛅) |  |  | 
FTIR Spec.: |  |  | 
Fourier Transform Infrared (FTIR)
Dynamic Shear Rheometer (DSR)
Bending Beam Rheometer (BBR)

## Slide 46: Binder Testing

## Slide 47: Phase 1 Outcomes:
Blending charts
  25%, 50%, and 70% RAP
  RA1 and RA2
Performance criteria comparison for each combination (rut depth and CT-index)
  Compare to control mix performance
Initial trends of mix design
Chemical IR comparison of blends to virgin
Binder property comparison

## Slide 48: Next Phase
Duplicates
  Results in BMD graph (rut vs. crack vs. rejuvenator dose)
100% RAP mix
RA3
Next phase determined with data trends

## Slide 49
Methodology
Notes: Speak out all points

## Slide 50: Standards and Process
Short Term Sample Conditioning -
  AASHTO T 324 => AASHTO R 30 => AASHTO 312
SuperPave Volumetric Mix Design - AASHTO M 323, R 35 -17
Theoretical Max Specific Gravity (Gmm) - AASHTO T 290-20
Superpave Gyratory Compactor - AASHTO T312-19
Hamburg Wheel Tracking Test - AASHTO T 324-19
Cracking Tolerance Index @ Intermediate Temperature - ASTM D8225 - 19

## Slide 51: Aggregate & RAP Batching
Virgin Preparation
  Sieved (Particle Size Distribution)
  ½”, ⅜”, No. 4, 8, 16, 30, 50, 100, 200, P200
RAP Preparation
  RAP- CA (> No.4), FA (<No.4)
  RAP mix, size down, and APEX

## Slide 52: Sample Preparation
Pre-conditioning - 2 hrs
Mixing
Conditioning - 4 hrs
Compaction
Volumetrics check
Testing
Notes: in order to eliminate segregation and clumping, each fraction (coarse and fine) RAP material was first split and mixed using a ribbon splitter, then was reduced in sample size using the splitter. Then, Using the APEX method, RAP CA and FA is weighed to the appropriate proportions.
RAP material was not sieved out all the way, just above and below the No. 4 sieve. This is due to variation between fine and coarse RAP particles and their available aged RAP binder for each.

## Slide 53: Performance Testing HWTT
HWTT:
  Rut depth (mm) < 10mm in 15,000 passes
  Rut resistance
  Stripping Inflection Point
  Permanent strain
    Creep & Damage stage of loading

## Slide 54: Performance Testing IDEAL-CT
CTindex
  Fracture Energy
  Applied Load
  Vertical deformation (mm)
  Sample Dimensions
Coefficient of Variation (COV)
Variation range
ANalysis Of VAriance (ANOVA)

## Slide 55: Performance Testing IDEAL-CT

## Slide 56
Preliminary Results
Notes: Speak out all points

## Slide 57: Virgin/Control Mix
HWTT:
No stripping
Under 4mm rut depth
Consistent results

## Slide 58: Virgin/Control Mix Cont.
IDEAL-CT
  CTindex = 89.7 (avg of 3)
  Above current ITD spec.
  Good control comparison
  Consistent

## Slide 59: Research Schedule

## Slide 60: Questions?
Notes: That’s why I have future research scope.